## Slide 1: Multi Objective Optimization

## Slide 2: Motivation

## Slide 3: Project goals
Develop an efficient numerical simulation for calculating a composite RVE equivalent elastic and thermal properties.
Construct a method for optimizing the microstructure of an RVE for a given set of elastic , thermal and density properties .

## Slide 4: Method summery
DOE
Gmsh
PBC
Mechanical simulation
Thermal simulation
Effective properties
RSM Model
Micromechanical
optimization

## Slide 5: Material Selection

## Slide 6: Material Selection
Name | Density | Modulus of elasticity | Failure strength | Elongation | Thermal Conductivity | Max service temp | Manufacturing
Ti-6av | 4.45 | 110 | 1170 | 10% | 7.1 | 900 | 3D,CNC
Glass | 2.5 | 70 | 40-250 | 4-5% | 0.2 | 400 | CNC?
Macor | 2.52 | 66.9 | 94 | 4-5% | 1.4 | 700 | CNC
Aluminum oxide | 3.9 | 350 | 460 | 0.1% | 30 | 1000 | ?
Zirconia | 5.6 | 200 | 330 | 0.2-0.3% | 3 | 500 | ?
Name | Density | Modulus of elasticity | Failure strength | Elongation | Thermal Conductivity | Max service temp | Manufacturing
Polyimide | 1.42 | 2.5 | 50-150 | 3% | 0.12 | 300 | Hot compression moulding
Cyanite ester | 1.2 | 2.9-4.3 | 50-150 | 5% | 0.2-0.4 | 350 | Casting
BMI | 1.2 | 3.5-4.5 | 50-150 | 4% | 0.3 | 250 | Casting

## Slide 7: RVE

## Slide 8: Geometry and design parameters

## Slide 9: Periodic BC

## Slide 10: Meshing – creating a periodic mesh

## Slide 11: Mechanical Simulation

## Slide 12: Thermal simulation

## Slide 13: Design space-1 parameter

## Slide 14: Design space-2 parameters

## Slide 15: Design space-3 parameters

## Slide 16: Design space-10 parameters

## Slide 17: RSM model-GPR vs NN

## Slide 18: RSM model-GPR vs NN
Regression Method | Rsq | RMSE | RUNTIME
GPR | 0.93 | 0.0495 | 900
NN | 0.91 | 0.0558 | 50

## Slide 19: RSM model-NN

## Slide 20: Objective Function

## Slide 21: Goal Optimization: case study
Goal-G12=2.21,K22=0.6,minimize weight
web | iso | Theta(0,0) | Theta(0,1) | Theta(0,2) | Theta(0,3) | Theta(1,0) | Theta(1,1) | Theta(1,2) | Theta(1,3)
1.02 | 0.358 | 142.3 | 38.7 | 133.2 | 40.7 | 140 | 136.65 | 137.6 | 49.6
 | rho | E11 | E22 | G12 | K11 | K22 | Obj | Best Obj
predicted | 2.05 | 4.88 | 4.62 | 2.65 | 0.687 | 0.451 | -4.61 | -2.86
simulated | 2.07 | 5.10 | 4.69 | 2.90 | 0.70 | 0.45 |  | 
Error |  |  |  |  |  |  |  | 

## Slide 22: Goal Optimization-sensitivity to objective parameters
 |  |  | [Tonne/m^3] | [GPa] | [GPa] | [GPa] | [W/mk] | [W/mk]
4 | 20 | 10 | 1.87 | 6.97 | 4.98 | 1.65 | 0.598 | 0.349
4 | 10 | 10 | 1.83 | 6.47 | 5.31 | 1.65 | 0.506 | 0.331
8 | 20 | 10 | 1.97 | 7.31 | 6.43 | 1.52 | 0.603 | 0.408
4 | 20 | 10 | 1.87 | 6.97 | 4.98 | 1.65 | 0.598 | 0.349
4 | 10 | 10 | 1.83 | 6.47 | 5.31 | 1.65 | 0.506 | 0.331
8 | 20 | 10 | 1.97 | 7.31 | 6.43 | 1.52 | 0.603 | 0.408

## Slide 23: Optimization using NSGA II
Random Population
Fitness evaluation
Stopping criteria
G
Selection
Crossover
Mutation
GA operators
Best Individual
New population
Yes
No
1
2
3
4
5
6
1
2
3
4
5
6
1
2
3
4
5
6

## Slide 24: Optimization using NSGA II
Generating random population
Assessing fitness value by frontiers
Assessing fitness using crowding distance

## Slide 25: E11 VS K11 DEMONSTRATION

## Slide 26: Optimization using NSGA II-Results